Technical specification for the tubing, pup joint,

X-over, flow coupling

Technical specification:

- All goods must fulfil the applicable ISO 11960 or API-Specification 5CT and 5B latest edition as well as Mill-Specification for gastight connection. CAL II and PSL 2 is require.

- All quoted OCTG must be new or in unused condition; joint lengths within Rg. 1, 2  if not otherwise specified.

- Grade of the material J – 55

- Required type of connection VAGT

- Tubing and pup joint with end-finishes with thread and coupling

- Threads completed with thread protector

List of required material:

| Item | OD | Nom Wt | Grade | Connect. | Remarks | Required delivery from order |
| --- | --- | --- | --- | --- | --- | --- |
|  | in | lb/ft |  | type |  |  |
| 1. | Tubing 2 3/8" | 4,60 | J 55 | VAGT | Rg. 1, 2 | 18-20 Weeks |
| 2. | Tubing 2 7/8" | 6,40 | J 55 | VAGT | Rg. 1, 2 | 18-20 Weeks |
| 3. | Tubing 3 1/2" | 9,20 | J 55 | VAGT | Rg. 1, 2 | 18-20 Weeks |
| 4. | Tubing 4 1/2" | 12,60 | J 55 | VAGT | Rg. 1, 2 | 18-20 Weeks |
| 5. | Pup Joint 2 3/8“ Length 1, 2, 3, 4 m | 4,60 | J 55 | VAGT |  | 18-20 Weeks |
| 6. | Pup Joint 2 7/8“ Length 1, 2, 3, 4 m | 6,40 | J 55 | VAGT |  | 18-20 Weeks |
| 7. | Pup Joint 3 1/2“ Length 1, 2, 3, 4 m | 9,20 | J 55 | VAGT |  | 18-20 Weeks |
| 8. | Pup Joint 4 1/2“ Length 1, 2, 3, 4 m | 12,60 | J 55 | VAGT |  | 18-20 Weeks |
| 9. | Coupling 2 7/8” | 6,40 | J 55 | VAGT |  | 18-20 Weeks |
| 10. | Coupling 3 ½” | 9,20 | J 55 | VAGT |  | 18-20 Weeks |
| 11. | Coupling 4 ½” | 12,60 | J 55 | VAGT |  | 18-20 Weeks |
| 12. | Flow coupling 4 ½” |  | J 55 | VAGT |  | 18-20 Weeks |
| 13. | Flow coupling 3 ½” |  | J 55 | VAGT |  | 18-20 Weeks |
| 14. | Crossover pin 2 7/8” x pin 3 ½” |  | J 55 | VAGT |  | 18-20 Weeks |
| 14. | Crossover pin 3 ½” x pin 4 ½” |  | J 55 | VAGT |  | 18-20 Weeks |

Documentation for delivery:

- Certificate of compliance stating that the material has been manufacured, sampled, tested and inspected in according API Specification 5 CT/ISO 11960,

- Mill and Material Test Certificate EN 10204/3.1,

- Documentation according API 5CT and 5B latest edition,

- Geometry, dimensions, drawings,

- Mechanical properties or efficiencies compared to the pipe body (tension, compression, bending),

- Pipe manufacturer (mill),

- Specifications of tubing connections (if not given by API 5CT).

Others requirements:

- One per year, supplier make training for the people of  the purchaser (approx. 10 people) with following schedule:

- Short introduction of the Company

- Principles of Connections

- (Thread / Seal /  Shoulder )

- Make-Up Graph

- Performance Properties

- Storage / Running

- Visual inspection & Field Repair.